Table S 1: Table showing outcome of all convergence cycles for each step of refinement process of RT WO3 subgroup candidates. Every candidate was optimised within 1% of the minimum Rwp at least 10 separate times in both steps.

| Subgroup Number | Lattice Refinement Cycles | Number of times within 1% Rwp of minimum | Full Optimisation Cycles | Number of times with 1% Rwp of minimum |
| --- | --- | --- | --- | --- |
| 5 | 2233 | 518 | 1500 | 1500 |
| 6 | 2055 | 1671 | 785 | 785 |
| 8 | 2255 | 514 | 1500 | 1500 |
| 9 | 1873 | 456 | 1492 | 1492 |
| 10 | 2371 | 552 | 914 | 914 |
| 11 | 2250 | 505 | 1500 | 1500 |
| 12 | 2064 | 497 | 300 | 300 |
| 13 | 2386 | 1359 | 1500 | 1500 |
| 14 | 2243 | 545 | 1500 | 1500 |
| 15 | 332 | 280 | 2360 | 2360 |
| 16 | 2047 | 1713 | 785 | 785 |
| 17 | 1984 | 1651 | 666 | 666 |
| 18 | 2370 | 583 | 929 | 929 |
| 19 | 1421 | 361 | 234 | 104 |
| 20 | 699 | 193 | 353 | 353 |
| 21 | 1486 | 876 | 127 | 127 |
| 22 | 1646 | 541 | 799 | 799 |
| 23 | 1858 | 356 | 1200 | 1200 |
| 24 | 1888 | 476 | 1543 | 1543 |
| 25 | 2228 | 603 | 260 | 251 |
| 26 | 2393 | 1309 | 1500 | 1500 |
| 27 | 1145 | 899 | 307 | 307 |
| 28 | 596 | 148 | 335 | 335 |
| 29 | 1027 | 198 | 146 | 146 |
| 30 | 1739 | 716 | 1085 | 1085 |
| 31 | 829 | 230 | 319 | 319 |
| 32 | 1309 | 239 | 324 | 324 |
| 33 | 750 | 294 | 126 | 126 |
| 34 | 2555 | 478 | 1147 | 1147 |
| 35 | 2233 | 552 | 1500 | 1500 |
| 36 | 2245 | 527 | 1500 | 1500 |
| 37 | 2248 | 541 | 1500 | 1500 |
| 38 | 2213 | 570 | 1500 | 1500 |
| 39 | 2212 | 546 | 1500 | 1500 |
| 40 | 1719 | 427 | 861 | 861 |
| 41 | 2353 | 578 | 1001 | 1001 |
| 42 | 2600 | 431 | 1122 | 1122 |
| 43 | 2270 | 536 | 1500 | 1500 |
| 44 | 2354 | 571 | 1006 | 1006 |
| 45 | 1713 | 452 | 860 | 860 |
| 46 | 1272 | 300 | 366 | 366 |
| 47 | 1794 | 399 | 642 | 642 |
| 48 | 1933 | 428 | 1767 | 1764 |
| 49 | 1870 | 480 | 1774 | 1774 |
| 50 | 2257 | 522 | 831 | 831 |
| 51 | 2367 | 613 | 856 | 856 |
| 52 | 2351 | 545 | 851 | 851 |
| 53 | 1742 | 452 | 722 | 722 |
| 54 | 2589 | 442 | 1134 | 1134 |
| 55 | 2167 | 563 | 1500 | 1500 |
| 56 | 1709 | 457 | 855 | 855 |
| 57 | 2364 | 577 | 992 | 992 |
| 58 | 2015 | 504 | 290 | 289 |
| 59 | 2054 | 541 | 263 | 263 |
| 60 | 2087 | 515 | 300 | 300 |
| 61 | 2252 | 616 | 277 | 273 |
| 62 | 219 | 48 | 184 | 153 |
| 63 | 1644 | 422 | 152 | 152 |
| 64 | 2305 | 1279 | 126 | 126 |
| 65 | 2371 | 1338 | 311 | 311 |
| 66 | 2389 | 1357 | 1500 | 1500 |
| 67 | 2394 | 1390 | 1497 | 1497 |
| 68 | 1510 | 279 | 858 | 858 |
| 69 | 1227 | 663 | 249 | 249 |
| 70 | 2579 | 467 | 1114 | 1114 |
| 71 | 2228 | 530 | 1500 | 1500 |
| 72 | 1718 | 465 | 839 | 839 |
| 73 | 2369 | 618 | 994 | 994 |
| 74 | 2274 | 506 | 830 | 830 |
| 75 | 1738 | 453 | 726 | 726 |
| 76 | 1211 | 282 | 160 | 118 |
| 77 | 774 | 210 | 172 | 172 |
| 78 | 1415 | 371 | 578 | 67 |
| 79 | 742 | 231 | 137 | 99 |
| 80 | 640 | 183 | 230 | 230 |
| 81 | 981 | 266 | 189 | 189 |
| 82 | 848 | 247 | 186 | 186 |
| 83 | 1092 | 212 | 271 | 190 |
| 84 | 1170 | 556 | 65 | 65 |
| 85 | 1431 | 863 | 215 | 215 |
| 86 | 1074 | 121 | 229 | 225 |
| 87 | 1248 | 701 | 141 | 140 |
| 88 | 1137 | 205 | 249 | 195 |
| 89 | 1500 | 869 | 126 | 126 |
| 90 | 1691 | 528 | 192 | 192 |
| 91 | 1888 | 613 | 547 | 547 |
| 92 | 960 | 239 | 213 | 194 |
| 93 | 565 | 129 | 127 | 125 |
| 94 | 1804 | 320 | 999 | 999 |
| 95 | 1691 | 314 | 219 | 219 |
| 96 | 1357 | 254 | 150 | 150 |
| 97 | 321 | 50 | 152 | 152 |
| 98 | 1695 | 337 | 515 | 515 |
| 99 | 2026 | 382 | 337 | 337 |
| 100 | 875 | 93 | 126 | 126 |
| 101 | 610 | 46 | 229 | 181 |
| 102 | 1264 | 308 | 359 | 359 |
| 103 | 1814 | 390 | 525 | 525 |
| 104 | 1810 | 437 | 237 | 233 |
| 105 | 1049 | 293 | 153 | 151 |
| 106 | 1889 | 502 | 231 | 230 |
| 107 | 2284 | 1297 | 126 | 126 |
| 108 | 1392 | 255 | 832 | 832 |
| 109 | 1252 | 644 | 241 | 241 |
| 110 | 643 | 163 | 136 | 119 |
| 111 | 686 | 143 | 159 | 159 |
| 112 | 389 | 70 | 86 | 86 |
| 113 | 947 | 176 | 136 | 136 |
| 114 | 694 | 55 | 113 | 104 |
| 115 | 907 | 101 | 70 | 54 |
| 116 | 1433 | 581 | 306 | 306 |
| 117 | 335 | 47 | 273 | 244 |
| 118 | 744 | 187 | 134 | 126 |
| 119 | 768 | 216 | 166 | 164 |
| 120 | 1203 | 222 | 103 | 103 |
| 121 | 439 | 78 | 120 | 120 |
| 122 | 1119 | 106 | 250 | 250 |
| 123 | 853 | 63 | 79 | 59 |
| 124 | 545 | 89 | 126 | 123 |
| 125 | 2156 | 519 | 285 | 285 |
| 126 | 2231 | 535 | 1309 | 1309 |
| 127 | 2193 | 739 | 971 | 971 |
| 128 | 2138 | 751 | 1230 | 1230 |
| 129 | 2249 | 520 | 1500 | 1500 |
| 130 | 2260 | 511 | 1500 | 1500 |
| 131 | 1702 | 280 | 825 | 825 |
| 132 | 2252 | 532 | 1500 | 1500 |
| 133 | 2112 | 546 | 285 | 285 |
| 134 | 2177 | 559 | 1312 | 1312 |
| 135 | 2122 | 771 | 968 | 968 |
| 136 | 1887 | 350 | 779 | 779 |
| 137 | 1071 | 187 | 475 | 475 |
| 138 | 1539 | 345 | 392 | 391 |
| 139 | 1050 | 269 | 580 | 580 |
| 140 | 1033 | 276 | 1362 | 1362 |
| 141 | 2073 | 490 | 520 | 520 |
| 142 | 2122 | 743 | 947 | 947 |
| 143 | 2075 | 760 | 831 | 831 |
| 144 | 1534 | 258 | 508 | 508 |
| 145 | 1833 | 670 | 513 | 513 |
| 146 | 1869 | 690 | 384 | 384 |
| 147 | 1674 | 289 | 820 | 820 |
| 148 | 2240 | 536 | 1500 | 1500 |
| 149 | 1755 | 462 | 208 | 207 |
| 150 | 2260 | 583 | 265 | 259 |
| 151 | 1707 | 471 | 170 | 168 |
| 152 | 2074 | 525 | 300 | 300 |
| 153 | 873 | 202 | 99 | 99 |
| 154 | 681 | 452 | 265 | 264 |
| 155 | 1858 | 1035 | 129 | 129 |
| 156 | 2373 | 1371 | 321 | 321 |
| 157 | 2251 | 1376 | 147 | 147 |
| 158 | 2408 | 1364 | 1500 | 1500 |
| 159 | 1917 | 333 | 115 | 98 |
| 160 | 1804 | 415 | 142 | 139 |
| 161 | 2171 | 514 | 285 | 285 |
| 162 | 2214 | 512 | 1310 | 1310 |
| 163 | 1904 | 346 | 756 | 756 |
| 164 | 2147 | 751 | 1239 | 1239 |
| 165 | 1796 | 640 | 615 | 615 |
| 166 | 1515 | 224 | 371 | 371 |
| 167 | 697 | 198 | 203 | 196 |
| 168 | 977 | 236 | 259 | 247 |
| 169 | 944 | 237 | 234 | 234 |
| 170 | 784 | 189 | 163 | 160 |
| 171 | 430 | 208 | 284 | 284 |
| 172 | 799 | 235 | 363 | 363 |
| 173 | 707 | 176 | 197 | 197 |
| 174 | 1158 | 218 | 75 | 75 |
| 175 | 1213 | 331 | 80 | 80 |
| 176 | 1415 | 886 | 160 | 160 |
| 177 | 1190 | 267 | 140 | 140 |
| 178 | 912 | 211 | 128 | 128 |
| 179 | 1186 | 231 | 221 | 143 |
| 180 | 1250 | 819 | 97 | 97 |
| 181 | 1418 | 416 | 205 | 205 |
| 182 | 1362 | 419 | 362 | 362 |
| 183 | 1052 | 331 | 94 | 94 |
| 184 | 899 | 63 | 302 | 302 |
| 185 | 1176 | 133 | 185 | 185 |
| 186 | 1564 | 354 | 187 | 187 |
| 187 | 1165 | 216 | 783 | 783 |
| 188 | 1042 | 144 | 120 | 120 |
| 189 | 1173 | 133 | 251 | 251 |
| 190 | 1259 | 165 | 169 | 169 |
| 191 | 788 | 61 | 223 | 220 |
| 192 | 544 | 36 | 119 | 119 |
| 193 | 1053 | 181 | 471 | 471 |
| 194 | 1140 | 301 | 389 | 389 |
| 195 | 1513 | 407 | 287 | 287 |
| 196 | 1300 | 323 | 192 | 183 |
| 197 | 964 | 241 | 231 | 231 |
| 198 | 1879 | 1041 | 127 | 127 |
| 199 | 1943 | 350 | 260 | 182 |
| 200 | 1869 | 478 | 147 | 147 |
| 201 | 607 | 39 | 142 | 122 |
| 202 | 691 | 190 | 186 | 186 |
| 203 | 723 | 87 | 119 | 119 |
| 204 | 685 | 116 | 124 | 121 |
| 205 | 591 | 42 | 83 | 83 |
| 206 | 709 | 44 | 193 | 193 |
| 207 | 1080 | 318 | 170 | 170 |
| 208 | 332 | 49 | 162 | 162 |
| 209 | 787 | 213 | 122 | 122 |
| 210 | 742 | 62 | 149 | 38 |
| 211 | 717 | 54 | 115 | 115 |
| 212 | 635 | 92 | 104 | 104 |
| 213 | 806 | 103 | 219 | 219 |
| 214 | 739 | 59 | 124 | 124 |
| 215 | 582 | 96 | 137 | 137 |
| 216 | 2668 | 1972 | 812 | 812 |
| 220 | 2676 | 1963 | 819 | 819 |
| 222 | 2682 | 2011 | 812 | 812 |
| 224 | 2709 | 2022 | 808 | 808 |
| 226 | 1868 | 410 | 203 | 203 |
| 227 | 2227 | 503 | 1204 | 1204 |
| 228 | 2177 | 726 | 1030 | 1030 |
| 229 | 2207 | 728 | 1028 | 1028 |
| 230 | 2284 | 517 | 1500 | 1500 |
| 231 | 2244 | 532 | 1500 | 1500 |
| 232 | 2166 | 461 | 984 | 984 |
| 233 | 2202 | 538 | 1500 | 1500 |
| 234 | 1694 | 1399 | 392 | 392 |
| 235 | 2014 | 1658 | 783 | 783 |
| 236 | 1907 | 1565 | 677 | 677 |
| 237 | 1923 | 1555 | 498 | 498 |
| 238 | 2692 | 2011 | 814 | 814 |
| 239 | 1810 | 425 | 200 | 200 |
| 240 | 2200 | 514 | 1205 | 1205 |
| 241 | 2189 | 665 | 1044 | 1044 |
| 242 | 2133 | 432 | 1024 | 1024 |
| 243 | 1030 | 242 | 418 | 418 |
| 244 | 1185 | 278 | 446 | 446 |
| 245 | 1126 | 282 | 438 | 438 |
| 246 | 1570 | 381 | 341 | 341 |
| 247 | 1914 | 466 | 406 | 406 |
| 248 | 2019 | 759 | 874 | 874 |
| 249 | 2070 | 750 | 833 | 833 |
| 250 | 1719 | 357 | 573 | 573 |
| 251 | 1573 | 431 | 464 | 464 |
| 252 | 1855 | 671 | 758 | 758 |
| 253 | 2214 | 472 | 976 | 976 |
| 254 | 2234 | 516 | 1500 | 1500 |
| 255 | 1306 | 328 | 109 | 109 |
| 256 | 1993 | 495 | 101 | 101 |
| 257 | 1736 | 461 | 177 | 177 |
| 258 | 2078 | 536 | 300 | 300 |
| 259 | 1874 | 503 | 276 | 276 |
| 260 | 2004 | 525 | 254 | 249 |
| 261 | 1593 | 900 | 138 | 138 |
| 262 | 2243 | 1358 | 167 | 167 |
| 263 | 2380 | 1326 | 1497 | 1497 |
| 264 | 2338 | 1270 | 718 | 718 |
| 265 | 1820 | 425 | 206 | 206 |
| 266 | 2188 | 524 | 1204 | 1204 |
| 267 | 2093 | 460 | 1037 | 1037 |
| 268 | 2208 | 703 | 1022 | 1022 |
| 269 | 783 | 325 | 224 | 218 |
| 270 | 1190 | 943 | 369 | 369 |
| 271 | 1477 | 1237 | 528 | 528 |
| 272 | 1943 | 1547 | 498 | 498 |
| 273 | 1401 | 1152 | 534 | 534 |
| 274 | 938 | 400 | 470 | 470 |
| 275 | 1642 | 484 | 544 | 544 |
| 276 | 1538 | 312 | 816 | 816 |
| 277 | 543 | 110 | 135 | 125 |
| 278 | 1084 | 319 | 159 | 138 |
| 279 | 936 | 211 | 182 | 182 |
| 280 | 602 | 152 | 111 | 58 |
| 281 | 759 | 195 | 135 | 135 |
| 282 | 1006 | 243 | 284 | 282 |
| 283 | 540 | 132 | 99 | 99 |
| 284 | 1188 | 682 | 129 | 129 |
| 285 | 1306 | 755 | 199 | 199 |
| 286 | 1291 | 854 | 100 | 100 |
| 287 | 1048 | 273 | 249 | 246 |
| 288 | 1175 | 300 | 382 | 382 |
| 289 | 1800 | 541 | 336 | 336 |
| 290 | 1442 | 327 | 244 | 244 |
| 291 | 875 | 71 | 148 | 145 |
| 292 | 968 | 117 | 136 | 132 |
| 293 | 1408 | 111 | 285 | 281 |
| 294 | 1077 | 109 | 349 | 349 |
| 295 | 1052 | 212 | 414 | 414 |
| 296 | 1186 | 315 | 347 | 347 |
| 297 | 1275 | 332 | 192 | 192 |
| 298 | 1753 | 503 | 267 | 267 |
| 299 | 944 | 223 | 240 | 240 |
| 300 | 1614 | 889 | 153 | 153 |
| 301 | 2081 | 1098 | 121 | 121 |
| 302 | 955 | 426 | 123 | 120 |
| 303 | 409 | 32 | 236 | 235 |
| 304 | 640 | 144 | 191 | 144 |
| 305 | 395 | 33 | 128 | 107 |
| 306 | 701 | 70 | 98 | 82 |
| 307 | 836 | 241 | 98 | 98 |
| 308 | 1331 | 375 | 433 | 433 |
| 309 | 640 | 150 | 171 | 154 |
| 310 | 461 | 97 | 225 | 223 |
| 311 | 725 | 68 | 163 | 163 |
| 312 | 565 | 36 | 148 | 148 |
| 313 | 296 | 79 | 94 | 89 |
| 314 | 2221 | 541 | 220 | 220 |
| 315 | 2115 | 801 | 1055 | 1055 |
| 316 | 2135 | 750 | 1147 | 1147 |
| 317 | 1968 | 686 | 652 | 652 |
| 318 | 2192 | 512 | 273 | 273 |
| 319 | 1477 | 271 | 220 | 220 |
| 320 | 1261 | 251 | 517 | 517 |
| 321 | 1602 | 321 | 604 | 604 |
| 322 | 2259 | 512 | 215 | 215 |
| 323 | 1304 | 615 | 273 | 273 |
| 324 | 1279 | 271 | 421 | 421 |
| 325 | 1528 | 311 | 594 | 594 |
| 326 | 1077 | 173 | 336 | 336 |
| 327 | 1040 | 343 | 367 | 367 |
| 328 | 1132 | 213 | 284 | 284 |
| 329 | 1050 | 184 | 451 | 451 |
| 330 | 1541 | 275 | 372 | 372 |
| 331 | 1410 | 250 | 282 | 282 |
| 332 | 1218 | 352 | 558 | 558 |
| 333 | 1777 | 658 | 702 | 702 |
| 334 | 1783 | 627 | 353 | 353 |
| 335 | 1715 | 672 | 373 | 373 |
| 336 | 1562 | 298 | 569 | 569 |
| 337 | 920 | 168 | 200 | 200 |
| 338 | 1313 | 334 | 184 | 182 |
| 339 | 1565 | 411 | 269 | 269 |
| 340 | 1040 | 279 | 299 | 299 |
| 341 | 118 | 30 | 106 | 101 |
| 342 | 1698 | 934 | 36 | 36 |
| 343 | 1837 | 1141 | 146 | 146 |
| 344 | 1525 | 892 | 155 | 155 |
| 345 | 2013 | 1146 | 194 | 194 |
| 346 | 2113 | 1172 | 360 | 360 |
| 347 | 1949 | 1151 | 226 | 226 |
| 348 | 2165 | 1237 | 182 | 182 |
| 349 | 1685 | 965 | 328 | 328 |
| 350 | 2242 | 1387 | 144 | 144 |
| 351 | 1746 | 1140 | 128 | 128 |
| 352 | 2286 | 1260 | 152 | 152 |
| 353 | 1287 | 103 | 112 | 112 |
| 354 | 1889 | 475 | 181 | 172 |
| 355 | 1187 | 188 | 448 | 231 |
| 356 | 1525 | 275 | 122 | 122 |
| 357 | 1205 | 385 | 124 | 117 |
| 358 | 1448 | 274 | 165 | 157 |
| 359 | 1569 | 424 | 106 | 106 |
| 360 | 1951 | 366 | 120 | 97 |
| 361 | 1353 | 227 | 217 | 170 |
| 362 | 1982 | 340 | 226 | 135 |
| 363 | 669 | 58 | 227 | 144 |
| 364 | 1562 | 272 | 1136 | 1136 |
| 365 | 1363 | 295 | 89 | 89 |
| 366 | 1368 | 131 | 158 | 158 |
| 367 | 1595 | 878 | 118 | 118 |
| 368 | 1863 | 998 | 127 | 127 |
| 369 | 1470 | 266 | 301 | 202 |
| 370 | 887 | 138 | 180 | 172 |
| 371 | 1489 | 243 | 480 | 278 |
| 372 | 1582 | 858 | 193 | 192 |
| 373 | 1134 | 89 | 97 | 89 |
| 374 | 1148 | 225 | 237 | 204 |
| 375 | 1027 | 255 | 209 | 140 |
| 376 | 1257 | 480 | 97 | 97 |
| 377 | 996 | 168 | 136 | 135 |
| 378 | 2255 | 491 | 219 | 219 |
| 379 | 1395 | 235 | 335 | 335 |
| 380 | 1323 | 269 | 525 | 525 |
| 381 | 1556 | 301 | 571 | 571 |
| 382 | 1372 | 354 | 384 | 384 |
| 383 | 1166 | 582 | 246 | 246 |
| 384 | 709 | 388 | 146 | 146 |
| 385 | 437 | 253 | 111 | 90 |
| 386 | 827 | 131 | 116 | 116 |
| 387 | 1020 | 90 | 133 | 132 |
| 388 | 940 | 70 | 110 | 109 |
| 389 | 911 | 103 | 105 | 105 |
| 390 | 1074 | 197 | 181 | 172 |
| 391 | 1106 | 304 | 133 | 130 |
| 392 | 1040 | 419 | 120 | 117 |
| 393 | 1025 | 108 | 133 | 133 |
| 394 | 861 | 195 | 93 | 91 |
| 395 | 948 | 259 | 131 | 131 |
| 396 | 619 | 135 | 132 | 129 |
| 397 | 763 | 176 | 168 | 168 |
| 398 | 965 | 253 | 124 | 124 |
| 399 | 917 | 318 | 129 | 129 |
| 400 | 778 | 192 | 166 | 143 |
| 401 | 933 | 181 | 132 | 132 |
| 402 | 1202 | 731 | 186 | 183 |
| 403 | 1041 | 197 | 119 | 119 |
| 404 | 1002 | 133 | 150 | 149 |
| 405 | 924 | 78 | 111 | 94 |
| 406 | 1093 | 225 | 258 | 179 |
| 407 | 1098 | 259 | 117 | 117 |
| 408 | 907 | 91 | 85 | 60 |
| 409 | 999 | 184 | 161 | 161 |
| 410 | 1167 | 224 | 144 | 144 |
| 411 | 1076 | 109 | 129 | 128 |
| 412 | 1090 | 114 | 117 | 117 |
| 413 | 863 | 238 | 144 | 144 |
| 414 | 855 | 84 | 279 | 279 |
| 415 | 548 | 79 | 114 | 92 |
| 416 | 1266 | 227 | 173 | 173 |
| 417 | 1416 | 271 | 115 | 115 |
| 418 | 1282 | 269 | 145 | 145 |
| 419 | 1180 | 241 | 139 | 139 |
| 420 | 1078 | 94 | 220 | 220 |
| 421 | 415 | 31 | 89 | 77 |
| 422 | 840 | 74 | 64 | 64 |
| 423 | 650 | 55 | 62 | 60 |
| 424 | 1084 | 172 | 102 | 102 |
| 425 | 652 | 79 | 64 | 62 |
| 426 | 261 | 17 | 94 | 81 |
| 427 | 285 | 39 | 90 | 90 |
| 428 | 960 | 102 | 159 | 159 |
| 429 | 864 | 65 | 87 | 86 |
| 430 | 476 | 42 | 99 | 99 |
| 431 | 304 | 25 | 162 | 140 |
| 432 | 1163 | 231 | 168 | 168 |
| 433 | 1354 | 235 | 214 | 214 |
| 434 | 1003 | 109 | 145 | 145 |
| 435 | 1103 | 96 | 143 | 143 |
| 436 | 439 | 35 | 92 | 77 |
| 437 | 413 | 36 | 145 | 145 |
| 438 | 561 | 32 | 87 | 79 |
| 439 | 757 | 103 | 109 | 108 |
| 440 | 685 | 65 | 118 | 118 |
| 441 | 511 | 89 | 97 | 82 |
| 442 | 1021 | 193 | 340 | 340 |
| 443 | 955 | 168 | 254 | 254 |
| 444 | 961 | 221 | 204 | 204 |
| 445 | 794 | 207 | 125 | 121 |
| 446 | 1715 | 944 | 35 | 35 |
| 447 | 1296 | 136 | 132 | 131 |
| 448 | 983 | 146 | 139 | 138 |
| 449 | 1533 | 262 | 176 | 130 |
| 450 | 1182 | 371 | 131 | 131 |
| 451 | 895 | 82 | 160 | 158 |
| 452 | 1305 | 227 | 161 | 158 |
| 453 | 1076 | 274 | 342 | 215 |
| 454 | 1307 | 310 | 162 | 162 |
| 455 | 798 | 174 | 116 | 116 |
| 456 | 481 | 82 | 175 | 162 |
| 457 | 446 | 36 | 96 | 96 |
| 458 | 526 | 46 | 92 | 91 |
| 459 | 701 | 51 | 97 | 96 |
| 460 | 692 | 65 | 94 | 94 |
| 461 | 573 | 96 | 117 | 114 |
| 462 | 669 | 61 | 110 | 99 |
| 463 | 526 | 45 | 125 | 120 |
| 464 | 944 | 363 | 117 | 117 |
| 465 | 246 | 21 | 104 | 96 |
| 466 | 240 | 33 | 97 | 97 |
| 467 | 610 | 51 | 121 | 113 |
| 468 | 897 | 78 | 143 | 143 |
| 469 | 548 | 54 | 67 | 65 |
| 470 | 352 | 35 | 72 | 71 |
| 471 | 411 | 24 | 84 | 77 |
| 472 | 766 | 123 | 118 | 118 |
| 473 | 432 | 30 | 109 | 109 |
| 474 | 638 | 91 | 118 | 110 |
| 475 | 429 | 65 | 102 | 98 |
| 476 | 1861 | 334 | 316 | 316 |
| 477 | 2083 | 392 | 130 | 130 |
| 478 | 2163 | 509 | 146 | 146 |
| 479 | 1973 | 361 | 125 | 125 |
| 480 | 1861 | 581 | 752 | 752 |
| 481 | 1840 | 602 | 750 | 750 |
| 482 | 2143 | 736 | 812 | 812 |
| 483 | 2114 | 701 | 784 | 784 |
| 484 | 1901 | 691 | 823 | 823 |
| 485 | 1960 | 683 | 288 | 288 |
| 486 | 2035 | 693 | 261 | 261 |
| 487 | 2056 | 726 | 460 | 460 |
| 488 | 1649 | 499 | 347 | 347 |
| 489 | 1914 | 711 | 907 | 907 |
| 490 | 1927 | 721 | 755 | 755 |
| 491 | 1589 | 492 | 413 | 413 |
| 492 | 2567 | 487 | 1063 | 1063 |
| 493 | 2572 | 469 | 1056 | 1056 |
| 494 | 2249 | 515 | 1500 | 1500 |
| 495 | 2263 | 513 | 1500 | 1500 |
| 496 | 1810 | 269 | 748 | 748 |
| 497 | 2597 | 469 | 1068 | 1068 |
| 498 | 1731 | 292 | 834 | 834 |
| 499 | 2158 | 447 | 981 | 981 |
| 500 | 2205 | 452 | 984 | 984 |
| 501 | 2250 | 512 | 1500 | 1500 |
| 502 | 2227 | 511 | 1500 | 1500 |
| 503 | 2185 | 444 | 976 | 976 |
| 504 | 1706 | 280 | 821 | 821 |
| 505 | 2249 | 519 | 1500 | 1500 |
| 506 | 1686 | 264 | 823 | 823 |
| 507 | 2236 | 521 | 1500 | 1500 |
| 508 | 2178 | 536 | 285 | 285 |
| 509 | 2217 | 525 | 1308 | 1308 |
| 510 | 2153 | 511 | 285 | 285 |
| 511 | 2197 | 517 | 1325 | 1325 |
| 512 | 2070 | 435 | 931 | 931 |
| 513 | 2137 | 769 | 1157 | 1157 |
| 514 | 2126 | 759 | 948 | 948 |
| 515 | 2122 | 433 | 959 | 959 |
| 516 | 468 | 115 | 279 | 279 |
| 517 | 1365 | 359 | 202 | 202 |
| 518 | 2056 | 513 | 714 | 714 |
| 519 | 1581 | 340 | 248 | 248 |
| 520 | 1655 | 572 | 757 | 757 |
| 521 | 1641 | 550 | 777 | 777 |
| 522 | 2070 | 794 | 965 | 965 |
| 523 | 2034 | 777 | 999 | 999 |
| 524 | 1818 | 454 | 200 | 200 |
| 525 | 2242 | 517 | 1206 | 1206 |
| 526 | 2209 | 541 | 1207 | 1207 |
| 527 | 1821 | 435 | 206 | 206 |
| 528 | 1895 | 320 | 862 | 862 |
| 529 | 2202 | 714 | 1008 | 1008 |
| 530 | 1880 | 312 | 820 | 820 |
| 531 | 2106 | 716 | 1028 | 1028 |
| 532 | 1675 | 522 | 797 | 797 |
| 533 | 1653 | 520 | 810 | 810 |
| 534 | 2064 | 776 | 970 | 970 |
| 535 | 2127 | 755 | 960 | 960 |
| 536 | 1447 | 223 | 348 | 348 |
| 537 | 1350 | 351 | 400 | 400 |
| 538 | 1519 | 256 | 446 | 446 |
| 539 | 1771 | 423 | 402 | 402 |
| 540 | 1901 | 346 | 328 | 328 |
| 541 | 2031 | 402 | 128 | 128 |
| 542 | 2169 | 534 | 146 | 146 |
| 543 | 1993 | 353 | 125 | 125 |
| 544 | 1840 | 619 | 756 | 756 |
| 545 | 1786 | 312 | 698 | 698 |
| 546 | 1949 | 407 | 877 | 877 |
| 547 | 1902 | 318 | 740 | 740 |
| 548 | 1795 | 673 | 765 | 765 |
| 549 | 1444 | 305 | 398 | 398 |
| 550 | 1164 | 284 | 336 | 336 |
| 551 | 1262 | 446 | 343 | 343 |
| 552 | 1547 | 509 | 344 | 344 |
| 553 | 1463 | 243 | 356 | 356 |
| 554 | 1306 | 456 | 283 | 283 |
| 555 | 1436 | 235 | 349 | 349 |
| 556 | 1036 | 170 | 218 | 218 |
| 557 | 1157 | 261 | 194 | 194 |
| 558 | 1125 | 198 | 358 | 358 |
| 559 | 1197 | 260 | 268 | 268 |
| 560 | 981 | 290 | 379 | 379 |
| 561 | 959 | 305 | 373 | 373 |
| 562 | 1041 | 275 | 433 | 433 |
| 563 | 1045 | 295 | 427 | 427 |
| 564 | 1048 | 178 | 407 | 407 |
| 565 | 1188 | 290 | 368 | 368 |
| 566 | 1031 | 170 | 404 | 404 |
| 567 | 1126 | 304 | 344 | 344 |
| 568 | 1068 | 232 | 396 | 396 |
| 569 | 1089 | 308 | 454 | 454 |
| 570 | 1089 | 311 | 391 | 391 |
| 571 | 1062 | 227 | 422 | 422 |
| 572 | 1568 | 313 | 163 | 163 |
| 573 | 1481 | 584 | 680 | 680 |
| 574 | 1711 | 642 | 495 | 495 |
| 575 | 1518 | 508 | 596 | 596 |
| 576 | 1426 | 551 | 656 | 656 |
| 577 | 1505 | 245 | 231 | 231 |
| 578 | 1503 | 331 | 319 | 319 |
| 579 | 1493 | 267 | 392 | 392 |
| 580 | 1730 | 619 | 625 | 625 |
| 581 | 1570 | 310 | 522 | 522 |
| 582 | 1454 | 352 | 273 | 273 |
| 583 | 1502 | 529 | 672 | 672 |
| 584 | 1537 | 484 | 372 | 372 |
| 585 | 1505 | 255 | 429 | 429 |
| 586 | 1457 | 545 | 719 | 719 |
| 587 | 1482 | 261 | 159 | 159 |
| 588 | 1396 | 385 | 397 | 396 |
| 589 | 1591 | 503 | 176 | 176 |
| 590 | 1764 | 591 | 360 | 360 |
| 591 | 1477 | 395 | 293 | 293 |
| 592 | 1804 | 283 | 753 | 753 |
| 593 | 2574 | 478 | 1062 | 1062 |
| 594 | 1731 | 274 | 830 | 830 |
| 595 | 2219 | 473 | 975 | 975 |
| 596 | 1255 | 286 | 301 | 301 |
| 597 | 1243 | 456 | 210 | 210 |
| 598 | 1736 | 649 | 533 | 533 |
| 599 | 1451 | 311 | 324 | 324 |
| 600 | 1442 | 230 | 357 | 357 |
| 601 | 1302 | 463 | 635 | 635 |
| 602 | 1502 | 252 | 428 | 428 |
| 603 | 1568 | 492 | 505 | 505 |
| 604 | 1185 | 283 | 182 | 176 |
| 605 | 1689 | 469 | 309 | 68 |
| 606 | 1375 | 369 | 94 | 89 |
| 607 | 1195 | 327 | 121 | 108 |
| 608 | 1338 | 344 | 206 | 204 |
| 609 | 1388 | 366 | 86 | 82 |
| 610 | 1478 | 374 | 283 | 282 |
| 611 | 1318 | 331 | 43 | 41 |
| 612 | 2012 | 564 | 191 | 191 |
| 613 | 1265 | 328 | 116 | 115 |
| 614 | 1989 | 497 | 286 | 286 |
| 615 | 676 | 130 | 174 | 174 |
| 616 | 2008 | 613 | 338 | 338 |
| 617 | 1488 | 384 | 204 | 202 |
| 618 | 1487 | 982 | 217 | 209 |
| 619 | 306 | 159 | 221 | 221 |
| 620 | 1109 | 239 | 151 | 151 |
| 621 | 1990 | 499 | 261 | 249 |
| 622 | 1060 | 281 | 152 | 152 |
| 623 | 691 | 442 | 269 | 268 |
| 624 | 1586 | 413 | 282 | 282 |
| 625 | 1913 | 573 | 249 | 249 |
| 626 | 275 | 73 | 172 | 159 |
| 627 | 958 | 281 | 200 | 194 |
| 628 | 927 | 225 | 181 | 181 |
| 629 | 671 | 171 | 116 | 116 |
| 630 | 443 | 109 | 147 | 141 |
| 631 | 990 | 252 | 137 | 135 |
| 632 | 1795 | 447 | 211 | 211 |
| 633 | 546 | 146 | 214 | 214 |
| 634 | 1254 | 321 | 178 | 177 |
| 635 | 1557 | 356 | 129 | 128 |
| 636 | 1054 | 309 | 130 | 126 |
| 637 | 622 | 145 | 195 | 159 |
| 638 | 1014 | 240 | 227 | 226 |
| 639 | 799 | 197 | 175 | 138 |
| 640 | 616 | 163 | 151 | 131 |
| 641 | 463 | 140 | 246 | 246 |
| 642 | 1240 | 309 | 161 | 161 |
| 643 | 755 | 171 | 167 | 166 |
| 644 | 1431 | 820 | 159 | 158 |
| 645 | 1780 | 1070 | 116 | 116 |
| 646 | 1448 | 868 | 138 | 138 |
| 647 | 1496 | 882 | 43 | 43 |
| 648 | 1575 | 973 | 124 | 124 |
| 649 | 1498 | 974 | 166 | 166 |
| 650 | 1729 | 1108 | 131 | 131 |
| 651 | 1410 | 856 | 115 | 115 |
| 652 | 1900 | 1158 | 52 | 52 |
| 653 | 1412 | 866 | 41 | 40 |
| 654 | 2277 | 1287 | 147 | 147 |
| 655 | 1190 | 216 | 210 | 121 |
| 656 | 2231 | 1219 | 344 | 344 |
| 657 | 1983 | 359 | 116 | 116 |
| 658 | 1608 | 389 | 110 | 110 |
| 659 | 1315 | 253 | 190 | 190 |
| 660 | 1790 | 500 | 112 | 112 |
| 661 | 2309 | 1195 | 717 | 717 |
| 662 | 1849 | 307 | 110 | 101 |
| 663 | 1846 | 470 | 144 | 138 |
| 664 | 1894 | 1039 | 128 | 128 |
| 665 | 2222 | 1150 | 111 | 111 |
| 666 | 975 | 159 | 363 | 344 |
| 667 | 1325 | 218 | 442 | 226 |
| 668 | 2095 | 1159 | 117 | 117 |
| 669 | 839 | 75 | 346 | 339 |
| 670 | 1069 | 180 | 227 | 195 |
| 671 | 959 | 315 | 95 | 95 |
| 672 | 1566 | 686 | 136 | 136 |
| 673 | 1600 | 918 | 109 | 109 |
| 674 | 1628 | 910 | 149 | 149 |
| 675 | 1844 | 332 | 115 | 115 |
| 676 | 1489 | 261 | 266 | 199 |
| 677 | 1104 | 311 | 114 | 114 |
| 678 | 1889 | 523 | 93 | 93 |
| 679 | 1079 | 203 | 100 | 100 |
| 680 | 1387 | 117 | 225 | 223 |
| 681 | 1623 | 923 | 146 | 146 |
| 682 | 1434 | 354 | 107 | 107 |
| 683 | 1109 | 216 | 84 | 64 |
| 684 | 1877 | 337 | 316 | 316 |
| 685 | 2109 | 440 | 129 | 129 |
| 686 | 2179 | 506 | 145 | 145 |
| 687 | 1973 | 352 | 123 | 123 |
| 688 | 1802 | 326 | 752 | 752 |
| 689 | 1827 | 620 | 751 | 751 |
| 690 | 1917 | 332 | 766 | 766 |
| 691 | 2009 | 418 | 802 | 802 |
| 692 | 1239 | 318 | 366 | 366 |
| 693 | 1229 | 415 | 225 | 225 |
| 694 | 1780 | 671 | 649 | 649 |
| 695 | 1501 | 297 | 479 | 479 |
| 696 | 1418 | 231 | 328 | 328 |
| 697 | 1271 | 463 | 611 | 611 |
| 698 | 1493 | 281 | 293 | 293 |
| 699 | 1543 | 493 | 575 | 575 |
| 700 | 929 | 270 | 144 | 144 |
| 701 | 1450 | 254 | 191 | 191 |
| 702 | 1244 | 311 | 284 | 284 |
| 703 | 1400 | 224 | 187 | 187 |
| 704 | 687 | 149 | 99 | 84 |
| 705 | 964 | 269 | 209 | 209 |
| 706 | 774 | 161 | 150 | 98 |
| 707 | 740 | 170 | 142 | 127 |
| 708 | 781 | 198 | 200 | 180 |
| 709 | 772 | 227 | 94 | 91 |
| 710 | 766 | 195 | 142 | 126 |
| 711 | 734 | 190 | 169 | 152 |
| 712 | 952 | 255 | 197 | 197 |
| 713 | 828 | 191 | 129 | 125 |
| 714 | 653 | 108 | 129 | 91 |
| 715 | 850 | 202 | 168 | 89 |
| 716 | 602 | 155 | 95 | 28 |
| 717 | 451 | 104 | 116 | 69 |
| 718 | 787 | 234 | 140 | 94 |
| 719 | 693 | 181 | 114 | 91 |
| 720 | 690 | 175 | 224 | 223 |
| 721 | 850 | 192 | 153 | 89 |
| 722 | 924 | 207 | 229 | 225 |
| 723 | 683 | 343 | 172 | 171 |
| 724 | 752 | 165 | 96 | 96 |
| 725 | 869 | 214 | 131 | 131 |
| 726 | 810 | 231 | 137 | 54 |
| 727 | 824 | 199 | 135 | 132 |
| 728 | 806 | 224 | 206 | 205 |
| 729 | 701 | 177 | 161 | 123 |
| 730 | 879 | 239 | 124 | 123 |
| 731 | 909 | 190 | 48 | 48 |
| 732 | 1041 | 432 | 86 | 85 |
| 733 | 935 | 230 | 111 | 104 |
| 734 | 1048 | 206 | 208 | 205 |
| 735 | 992 | 95 | 132 | 70 |
| 736 | 1133 | 464 | 133 | 133 |
| 737 | 1058 | 353 | 147 | 147 |
| 738 | 1119 | 214 | 127 | 125 |
| 739 | 1103 | 294 | 151 | 151 |
| 740 | 906 | 62 | 133 | 133 |
| 741 | 962 | 197 | 110 | 110 |
| 742 | 1146 | 640 | 158 | 158 |
| 743 | 1180 | 347 | 102 | 99 |
| 744 | 1112 | 114 | 103 | 102 |
| 745 | 852 | 145 | 104 | 99 |
| 746 | 954 | 169 | 128 | 128 |
| 747 | 1039 | 170 | 148 | 148 |
| 748 | 870 | 171 | 136 | 136 |
| 749 | 884 | 221 | 142 | 142 |
| 750 | 1068 | 639 | 156 | 153 |
| 751 | 1062 | 116 | 180 | 178 |
| 752 | 1082 | 111 | 151 | 151 |
| 753 | 968 | 270 | 141 | 141 |
| 754 | 1169 | 207 | 210 | 210 |
| 755 | 1200 | 661 | 130 | 130 |
| 756 | 902 | 304 | 275 | 272 |
| 757 | 941 | 239 | 212 | 204 |
| 758 | 1007 | 327 | 225 | 223 |
| 759 | 958 | 323 | 161 | 146 |
| 760 | 867 | 261 | 350 | 350 |
| 761 | 380 | 28 | 316 | 316 |
| 762 | 547 | 84 | 284 | 284 |
| 763 | 909 | 60 | 296 | 296 |
| 764 | 963 | 201 | 140 | 126 |
| 765 | 511 | 123 | 129 | 126 |
| 766 | 463 | 121 | 152 | 149 |
| 767 | 812 | 150 | 93 | 75 |
| 768 | 703 | 171 | 151 | 136 |
| 769 | 525 | 124 | 126 | 125 |
| 770 | 707 | 121 | 207 | 198 |
| 771 | 403 | 94 | 203 | 153 |
| 772 | 1013 | 136 | 62 | 49 |
| 773 | 1024 | 239 | 135 | 126 |
| 774 | 965 | 149 | 46 | 44 |
| 775 | 852 | 206 | 104 | 103 |
| 776 | 1254 | 229 | 472 | 472 |
| 777 | 538 | 63 | 176 | 176 |
| 778 | 614 | 121 | 538 | 538 |
| 779 | 941 | 125 | 115 | 115 |
| 780 | 1052 | 126 | 164 | 164 |
| 781 | 430 | 120 | 146 | 146 |
| 782 | 274 | 30 | 47 | 47 |
| 783 | 463 | 97 | 205 | 205 |
| 784 | 238 | 44 | 141 | 122 |
| 785 | 919 | 100 | 48 | 47 |
| 786 | 365 | 55 | 128 | 123 |
| 787 | 267 | 24 | 75 | 66 |
| 788 | 935 | 164 | 129 | 80 |
| 789 | 1061 | 197 | 75 | 75 |
| 790 | 1034 | 177 | 77 | 56 |
| 791 | 963 | 169 | 129 | 112 |
| 792 | 1186 | 83 | 170 | 170 |
| 793 | 610 | 55 | 163 | 159 |
| 794 | 1006 | 96 | 285 | 285 |
| 795 | 580 | 45 | 147 | 147 |
| 796 | 503 | 57 | 90 | 89 |
| 797 | 771 | 55 | 64 | 54 |
| 798 | 249 | 18 | 100 | 84 |
| 799 | 699 | 45 | 72 | 49 |
| 800 | 894 | 81 | 69 | 68 |
| 801 | 618 | 51 | 70 | 70 |
| 802 | 602 | 41 | 89 | 87 |
| 803 | 433 | 26 | 70 | 62 |
| 804 | 1067 | 185 | 203 | 203 |
| 805 | 916 | 259 | 220 | 220 |
| 806 | 1055 | 178 | 194 | 194 |
| 807 | 1144 | 224 | 281 | 281 |
| 808 | 1056 | 269 | 77 | 69 |
| 809 | 1141 | 238 | 212 | 212 |
| 810 | 888 | 231 | 182 | 174 |
| 811 | 906 | 212 | 180 | 174 |
| 812 | 960 | 239 | 162 | 89 |
| 813 | 872 | 246 | 135 | 131 |
| 814 | 711 | 150 | 119 | 112 |
| 815 | 917 | 211 | 137 | 134 |
| 816 | 1363 | 329 | 152 | 152 |
| 817 | 942 | 229 | 99 | 98 |
| 818 | 1442 | 801 | 165 | 165 |
| 819 | 1378 | 250 | 241 | 241 |
| 820 | 1346 | 235 | 144 | 144 |
| 821 | 1203 | 313 | 150 | 146 |
| 822 | 1676 | 434 | 109 | 109 |
| 823 | 1159 | 232 | 172 | 172 |
| 824 | 1369 | 128 | 191 | 191 |
| 825 | 1129 | 190 | 124 | 121 |
| 826 | 1431 | 565 | 144 | 144 |
| 827 | 1047 | 233 | 108 | 108 |
| 828 | 523 | 123 | 118 | 101 |
| 829 | 533 | 61 | 144 | 130 |
| 830 | 512 | 109 | 104 | 98 |
| 831 | 567 | 135 | 103 | 101 |
| 832 | 506 | 64 | 58 | 56 |
| 833 | 601 | 94 | 77 | 63 |
| 834 | 735 | 86 | 71 | 66 |
| 835 | 514 | 77 | 85 | 50 |
| 836 | 505 | 29 | 86 | 74 |
| 837 | 558 | 45 | 74 | 70 |
| 838 | 487 | 41 | 73 | 59 |
| 839 | 474 | 37 | 97 | 75 |
| 840 | 763 | 222 | 44 | 40 |
| 841 | 470 | 79 | 127 | 127 |
| 842 | 306 | 34 | 109 | 96 |
| 843 | 261 | 26 | 112 | 110 |
| 844 | 609 | 77 | 117 | 84 |
| 845 | 396 | 116 | 89 | 73 |
| 846 | 648 | 147 | 109 | 106 |
| 847 | 625 | 153 | 113 | 108 |
| 848 | 815 | 75 | 65 | 54 |
| 849 | 515 | 53 | 70 | 67 |
| 850 | 669 | 36 | 39 | 24 |
| 851 | 424 | 38 | 67 | 29 |
| 852 | 730 | 62 | 104 | 93 |
| 853 | 480 | 30 | 106 | 106 |
| 854 | 604 | 53 | 98 | 89 |
| 855 | 464 | 51 | 95 | 80 |
| 856 | 387 | 49 | 113 | 111 |
| 857 | 2492 | 1830 | 1197 | 1197 |
| 858 | 2409 | 1806 | 794 | 794 |
| 859 | 2508 | 1861 | 1197 | 1197 |
| 860 | 1044 | 782 | 513 | 513 |
| 861 | 2488 | 1865 | 1173 | 1173 |
| 862 | 2375 | 1803 | 979 | 979 |
| 863 | 2261 | 1736 | 527 | 527 |
| 864 | 2465 | 1824 | 1197 | 1197 |
| 865 | 2386 | 1789 | 795 | 795 |
| 866 | 2117 | 423 | 202 | 202 |
| 867 | 1938 | 663 | 618 | 618 |
| 868 | 1634 | 625 | 260 | 260 |
| 869 | 1752 | 522 | 550 | 550 |
| 870 | 2138 | 506 | 285 | 285 |
| 871 | 1615 | 308 | 290 | 290 |
| 872 | 1086 | 165 | 315 | 314 |
| 873 | 1414 | 264 | 583 | 583 |
| 874 | 1491 | 1082 | 359 | 359 |
| 875 | 2520 | 1849 | 1174 | 1174 |
| 876 | 1147 | 889 | 899 | 899 |
| 877 | 1100 | 810 | 564 | 564 |
| 878 | 2110 | 438 | 202 | 202 |
| 879 | 1373 | 381 | 422 | 422 |
| 880 | 971 | 160 | 228 | 228 |
| 881 | 1234 | 203 | 353 | 353 |
| 882 | 1139 | 177 | 352 | 352 |
| 883 | 923 | 243 | 384 | 384 |
| 884 | 1137 | 194 | 377 | 377 |
| 885 | 1019 | 179 | 448 | 448 |
| 886 | 1411 | 260 | 321 | 321 |
| 887 | 1373 | 219 | 191 | 191 |
| 888 | 1225 | 393 | 311 | 311 |
| 889 | 1721 | 692 | 723 | 723 |
| 890 | 1621 | 485 | 315 | 315 |
| 891 | 1317 | 527 | 223 | 223 |
| 892 | 1519 | 299 | 424 | 424 |
| 893 | 1293 | 222 | 269 | 269 |
| 894 | 1398 | 362 | 114 | 114 |
| 895 | 1377 | 391 | 160 | 160 |
| 896 | 754 | 169 | 166 | 166 |
| 897 | 310 | 78 | 165 | 165 |
| 898 | 1422 | 815 | 147 | 147 |
| 899 | 1438 | 875 | 124 | 124 |
| 900 | 1530 | 902 | 147 | 147 |
| 901 | 1605 | 987 | 141 | 141 |
| 902 | 2005 | 1207 | 300 | 300 |
| 903 | 1366 | 941 | 158 | 158 |
| 904 | 1876 | 1032 | 128 | 128 |
| 905 | 1247 | 264 | 58 | 58 |
| 906 | 1894 | 468 | 196 | 195 |
| 907 | 1955 | 339 | 124 | 124 |
| 908 | 617 | 118 | 67 | 67 |
| 909 | 1498 | 292 | 108 | 108 |
| 910 | 1679 | 617 | 188 | 188 |
| 911 | 1821 | 313 | 121 | 121 |
| 912 | 1495 | 563 | 216 | 216 |
| 913 | 1425 | 553 | 132 | 132 |
| 914 | 2128 | 451 | 202 | 202 |
| 915 | 1421 | 374 | 401 | 401 |
| 916 | 1291 | 194 | 155 | 155 |
| 917 | 1395 | 285 | 409 | 409 |
| 918 | 704 | 455 | 213 | 211 |
| 919 | 1373 | 778 | 282 | 282 |
| 920 | 814 | 647 | 364 | 364 |
| 921 | 1129 | 301 | 308 | 308 |
| 922 | 1041 | 155 | 252 | 252 |
| 923 | 756 | 186 | 172 | 170 |
| 924 | 619 | 167 | 145 | 145 |
| 925 | 580 | 137 | 121 | 121 |
| 926 | 800 | 177 | 92 | 91 |
| 927 | 996 | 225 | 113 | 112 |
| 928 | 1110 | 225 | 131 | 130 |
| 929 | 988 | 145 | 144 | 144 |
| 930 | 1005 | 380 | 134 | 133 |
| 931 | 1111 | 229 | 124 | 124 |
| 932 | 1113 | 448 | 179 | 179 |
| 933 | 1079 | 405 | 171 | 168 |
| 934 | 1087 | 237 | 122 | 122 |
| 935 | 1048 | 436 | 136 | 136 |
| 936 | 937 | 268 | 75 | 73 |
| 937 | 1046 | 339 | 186 | 45 |
| 938 | 368 | 29 | 182 | 182 |
| 939 | 774 | 109 | 120 | 118 |
| 940 | 816 | 145 | 156 | 155 |
| 941 | 754 | 123 | 182 | 144 |
| 942 | 701 | 61 | 324 | 321 |
| 943 | 352 | 40 | 193 | 191 |
| 944 | 481 | 42 | 121 | 121 |
| 945 | 669 | 93 | 218 | 216 |
| 946 | 562 | 103 | 179 | 178 |
| 947 | 455 | 46 | 111 | 109 |
| 948 | 419 | 68 | 117 | 117 |
| 949 | 997 | 182 | 296 | 296 |
| 950 | 884 | 133 | 251 | 251 |
| 951 | 917 | 228 | 195 | 195 |
| 952 | 382 | 86 | 125 | 125 |
| 953 | 1408 | 812 | 144 | 144 |
| 954 | 1318 | 334 | 123 | 123 |
| 955 | 1105 | 206 | 150 | 150 |
| 956 | 1289 | 278 | 119 | 119 |
| 957 | 1543 | 846 | 197 | 197 |
| 958 | 1187 | 664 | 136 | 136 |
| 959 | 331 | 125 | 173 | 173 |
| 960 | 414 | 22 | 143 | 125 |
| 961 | 382 | 49 | 139 | 137 |
| 962 | 541 | 40 | 142 | 142 |
| 963 | 509 | 74 | 150 | 140 |
| 964 | 659 | 80 | 118 | 118 |
| 965 | 339 | 57 | 113 | 113 |
| 966 | 494 | 24 | 88 | 72 |
| 967 | 673 | 78 | 110 | 100 |
| 968 | 386 | 22 | 170 | 169 |
| 969 | 466 | 66 | 154 | 148 |
| 970 | 373 | 55 | 76 | 73 |
| 971 | 2262 | 1678 | 271 | 271 |
| 972 | 2393 | 1802 | 799 | 799 |
| 973 | 2227 | 1684 | 855 | 855 |
| 974 | 2471 | 1860 | 1197 | 1197 |
| 975 | 2499 | 1839 | 1197 | 1197 |
| 976 | 1715 | 1286 | 152 | 152 |
| 977 | 2174 | 1662 | 845 | 845 |
| 978 | 2501 | 1867 | 1197 | 1197 |
| 979 | 2268 | 1667 | 271 | 271 |
| 980 | 1095 | 806 | 508 | 508 |
| 981 | 557 | 429 | 175 | 161 |
| 982 | 2477 | 1838 | 1197 | 1197 |
| 983 | 2175 | 1581 | 256 | 256 |
| 984 | 2120 | 1582 | 789 | 789 |
| 985 | 2106 | 1588 | 653 | 653 |
| 986 | 2490 | 1821 | 1194 | 1194 |
| 987 | 1337 | 1022 | 187 | 187 |
| 988 | 251 | 188 | 240 | 240 |
| 989 | 2265 | 1677 | 290 | 290 |
| 990 | 1692 | 1256 | 142 | 142 |
| 991 | 2143 | 1625 | 696 | 696 |
| 992 | 2476 | 1851 | 1197 | 1197 |
| 993 | 1560 | 297 | 153 | 148 |
| 994 | 1831 | 395 | 170 | 170 |
| 995 | 1378 | 451 | 453 | 453 |
| 996 | 1561 | 527 | 435 | 435 |
| 997 | 1761 | 658 | 481 | 481 |
| 998 | 1686 | 631 | 427 | 427 |
| 999 | 1400 | 558 | 139 | 139 |
| 1000 | 1181 | 451 | 142 | 142 |
| 1001 | 1150 | 444 | 272 | 272 |
| 1002 | 1392 | 551 | 309 | 309 |
| 1003 | 1320 | 351 | 470 | 470 |
| 1004 | 1730 | 658 | 316 | 316 |
| 1005 | 1515 | 575 | 269 | 269 |
| 1006 | 1307 | 434 | 133 | 133 |
| 1007 | 1565 | 497 | 335 | 335 |
| 1008 | 1610 | 528 | 345 | 345 |
| 1009 | 2221 | 530 | 225 | 225 |
| 1010 | 2208 | 494 | 223 | 223 |
| 1011 | 1414 | 289 | 594 | 594 |
| 1012 | 1332 | 228 | 514 | 514 |
| 1013 | 830 | 146 | 282 | 282 |
| 1014 | 1541 | 266 | 268 | 268 |
| 1015 | 1223 | 187 | 364 | 364 |
| 1016 | 1445 | 230 | 304 | 304 |
| 1017 | 1542 | 259 | 426 | 426 |
| 1018 | 1341 | 198 | 371 | 371 |
| 1019 | 1524 | 290 | 528 | 528 |
| 1020 | 1514 | 300 | 484 | 484 |
| 1021 | 1380 | 242 | 377 | 377 |
| 1022 | 1625 | 327 | 680 | 680 |
| 1023 | 1181 | 282 | 326 | 326 |
| 1024 | 1825 | 653 | 781 | 781 |
| 1025 | 1807 | 290 | 347 | 347 |
| 1026 | 2148 | 485 | 142 | 142 |
| 1027 | 627 | 141 | 186 | 186 |
| 1028 | 1017 | 203 | 294 | 294 |
| 1029 | 1504 | 268 | 317 | 317 |
| 1030 | 1546 | 286 | 320 | 320 |
| 1031 | 1105 | 172 | 209 | 209 |
| 1032 | 917 | 145 | 176 | 176 |
| 1033 | 1086 | 194 | 107 | 103 |
| 1034 | 829 | 133 | 115 | 115 |
| 1035 | 1447 | 255 | 271 | 271 |
| 1036 | 1171 | 174 | 186 | 186 |
| 1037 | 1279 | 221 | 118 | 118 |
| 1038 | 1239 | 206 | 109 | 109 |
| 1039 | 1559 | 301 | 497 | 497 |
| 1040 | 1548 | 306 | 529 | 529 |
| 1041 | 2085 | 411 | 207 | 207 |
| 1042 | 2049 | 439 | 209 | 209 |
| 1043 | 1313 | 246 | 298 | 298 |
| 1044 | 1273 | 249 | 194 | 194 |
| 1045 | 1150 | 262 | 263 | 263 |
| 1046 | 1780 | 674 | 635 | 635 |
| 1047 | 1013 | 313 | 86 | 86 |
| 1048 | 1215 | 431 | 137 | 137 |
| 1049 | 1221 | 229 | 148 | 147 |
| 1050 | 1085 | 174 | 137 | 118 |
| 1051 | 1480 | 337 | 630 | 630 |
| 1052 | 1418 | 375 | 614 | 614 |
| 1053 | 829 | 115 | 148 | 60 |
| 1054 | 1373 | 247 | 150 | 150 |
| 1055 | 1318 | 238 | 344 | 344 |
| 1056 | 1570 | 254 | 418 | 418 |
| 1057 | 1202 | 724 | 199 | 199 |
| 1058 | 1096 | 533 | 187 | 168 |
| 1059 | 1191 | 570 | 114 | 112 |
| 1060 | 1520 | 1135 | 264 | 264 |
| 1061 | 2141 | 1619 | 243 | 243 |
| 1062 | 590 | 410 | 153 | 144 |
| 1063 | 893 | 697 | 147 | 55 |
| 1064 | 1574 | 316 | 149 | 148 |
| 1065 | 1823 | 444 | 161 | 161 |
| 1066 | 814 | 124 | 155 | 155 |
| 1067 | 1096 | 179 | 230 | 230 |
| 1068 | 1266 | 422 | 370 | 370 |
| 1069 | 1140 | 174 | 349 | 349 |
| 1070 | 993 | 150 | 174 | 174 |
| 1071 | 433 | 69 | 132 | 129 |
| 1072 | 848 | 407 | 118 | 92 |
| 1073 | 952 | 451 | 171 | 171 |
| 1074 | 1217 | 291 | 140 | 140 |
| 1075 | 1119 | 278 | 211 | 211 |
| 1076 | 1090 | 492 | 170 | 170 |
| 1077 | 871 | 147 | 147 | 145 |
| 1078 | 1339 | 347 | 215 | 215 |
| 1079 | 1293 | 234 | 290 | 290 |
| 1080 | 927 | 170 | 155 | 75 |
| 1081 | 1003 | 184 | 337 | 337 |
| 1082 | 783 | 209 | 126 | 105 |
| 1083 | 834 | 141 | 189 | 189 |
| 1084 | 947 | 125 | 139 | 54 |
| 1085 | 861 | 140 | 156 | 51 |
| 1086 | 1058 | 195 | 175 | 166 |
| 1087 | 1048 | 176 | 311 | 311 |
| 1088 | 999 | 184 | 311 | 311 |
| 1089 | 1085 | 156 | 232 | 232 |
| 1090 | 921 | 165 | 206 | 206 |
| 1091 | 865 | 219 | 192 | 192 |
| 1092 | 949 | 164 | 185 | 184 |
| 1093 | 1114 | 159 | 201 | 200 |
| 1094 | 1078 | 187 | 276 | 276 |
| 1095 | 1009 | 195 | 240 | 240 |
| 1096 | 1307 | 205 | 98 | 65 |
| 1097 | 1349 | 378 | 312 | 312 |
| 1098 | 1153 | 178 | 122 | 96 |
| 1099 | 1138 | 188 | 157 | 157 |
| 1100 | 982 | 262 | 247 | 247 |
| 1101 | 994 | 164 | 197 | 197 |
| 1102 | 893 | 274 | 242 | 242 |
| 1103 | 1155 | 305 | 358 | 358 |
| 1104 | 1342 | 368 | 277 | 277 |
| 1105 | 1096 | 155 | 135 | 135 |
| 1106 | 1097 | 172 | 118 | 111 |
| 1107 | 1200 | 175 | 109 | 94 |
| 1108 | 947 | 144 | 152 | 152 |
| 1109 | 926 | 258 | 160 | 153 |
| 1110 | 1126 | 317 | 304 | 304 |
| 1111 | 1348 | 312 | 265 | 265 |
| 1112 | 1032 | 286 | 192 | 57 |
| 1113 | 894 | 324 | 223 | 223 |
| 1114 | 1202 | 374 | 130 | 127 |
| 1115 | 835 | 295 | 216 | 216 |
| 1116 | 1186 | 190 | 256 | 256 |
| 1117 | 1398 | 209 | 287 | 287 |
| 1118 | 1259 | 396 | 245 | 245 |
| 1119 | 1325 | 207 | 298 | 298 |
| 1120 | 1274 | 276 | 273 | 273 |
| 1121 | 996 | 146 | 108 | 104 |
| 1122 | 1190 | 244 | 214 | 214 |
| 1123 | 916 | 135 | 67 | 67 |
| 1124 | 1240 | 198 | 319 | 319 |
| 1125 | 1037 | 170 | 118 | 108 |
| 1126 | 1303 | 361 | 387 | 387 |
| 1127 | 1109 | 188 | 102 | 74 |
| 1128 | 1031 | 257 | 109 | 87 |
| 1129 | 1085 | 293 | 126 | 107 |
| 1130 | 1039 | 273 | 141 | 117 |
| 1131 | 1149 | 324 | 86 | 82 |
| 1132 | 1087 | 302 | 150 | 80 |
| 1133 | 1112 | 321 | 134 | 134 |
| 1134 | 937 | 265 | 212 | 212 |
| 1135 | 680 | 161 | 132 | 106 |
| 1136 | 348 | 73 | 179 | 179 |
| 1137 | 515 | 124 | 146 | 143 |
| 1138 | 849 | 213 | 150 | 150 |
| 1139 | 410 | 87 | 142 | 142 |
| 1140 | 964 | 226 | 136 | 130 |
| 1141 | 323 | 93 | 84 | 84 |
| 1142 | 305 | 84 | 94 | 77 |
| 1143 | 638 | 153 | 148 | 145 |
| 1144 | 909 | 224 | 122 | 120 |
| 1145 | 499 | 119 | 86 | 33 |
| 1146 | 1016 | 258 | 180 | 180 |
| 1147 | 753 | 186 | 160 | 132 |
| 1148 | 897 | 209 | 112 | 104 |
| 1149 | 382 | 93 | 100 | 56 |
| 1150 | 679 | 156 | 136 | 136 |
| 1151 | 536 | 132 | 112 | 98 |
| 1152 | 1168 | 630 | 66 | 66 |
| 1153 | 1275 | 525 | 130 | 130 |
| 1154 | 1074 | 560 | 147 | 147 |
| 1155 | 1085 | 634 | 83 | 83 |
| 1156 | 1141 | 670 | 141 | 141 |
| 1157 | 1038 | 406 | 105 | 104 |
| 1158 | 1162 | 777 | 131 | 131 |
| 1159 | 994 | 689 | 59 | 59 |
| 1160 | 998 | 680 | 121 | 119 |
| 1161 | 1387 | 849 | 131 | 131 |
| 1162 | 1246 | 788 | 153 | 153 |
| 1163 | 1100 | 705 | 156 | 156 |
| 1164 | 1078 | 692 | 139 | 139 |
| 1165 | 1235 | 762 | 100 | 100 |
| 1166 | 1144 | 747 | 128 | 127 |
| 1167 | 1073 | 748 | 86 | 83 |
| 1168 | 1737 | 978 | 29 | 29 |
| 1169 | 831 | 144 | 105 | 105 |
| 1170 | 1335 | 240 | 204 | 204 |
| 1171 | 1205 | 391 | 96 | 95 |
| 1172 | 1111 | 203 | 136 | 133 |
| 1173 | 1117 | 249 | 125 | 121 |
| 1174 | 1112 | 87 | 73 | 73 |
| 1175 | 1246 | 113 | 184 | 184 |
| 1176 | 963 | 92 | 98 | 85 |
| 1177 | 1009 | 90 | 96 | 88 |
| 1178 | 1645 | 381 | 203 | 203 |
| 1179 | 1041 | 461 | 103 | 103 |
| 1180 | 1263 | 239 | 139 | 139 |
| 1181 | 1051 | 199 | 112 | 112 |
| 1182 | 1478 | 305 | 180 | 179 |
| 1183 | 1520 | 362 | 101 | 101 |
| 1184 | 1539 | 674 | 252 | 252 |
| 1185 | 1289 | 289 | 101 | 101 |
| 1186 | 1541 | 298 | 151 | 151 |
| 1187 | 1005 | 74 | 111 | 111 |
| 1188 | 1063 | 341 | 159 | 158 |
| 1189 | 1305 | 112 | 152 | 152 |
| 1190 | 1296 | 128 | 121 | 120 |
| 1191 | 1292 | 109 | 140 | 140 |
| 1192 | 1246 | 135 | 159 | 157 |
| 1193 | 754 | 56 | 173 | 173 |
| 1194 | 1370 | 332 | 75 | 75 |
| 1195 | 998 | 201 | 106 | 104 |
| 1196 | 1494 | 525 | 201 | 201 |
| 1197 | 1125 | 411 | 118 | 118 |
| 1198 | 1312 | 482 | 174 | 174 |
| 1199 | 1467 | 542 | 111 | 110 |
| 1200 | 892 | 151 | 218 | 201 |
| 1201 | 829 | 144 | 137 | 137 |
| 1202 | 1288 | 121 | 225 | 225 |
| 1203 | 1325 | 124 | 139 | 139 |
| 1204 | 1450 | 818 | 162 | 162 |
| 1205 | 1230 | 394 | 162 | 162 |
| 1206 | 1274 | 122 | 169 | 168 |
| 1207 | 923 | 161 | 61 | 60 |
| 1208 | 1337 | 357 | 107 | 107 |
| 1209 | 998 | 233 | 138 | 136 |
| 1210 | 1147 | 287 | 165 | 165 |
| 1211 | 1085 | 295 | 98 | 98 |
| 1212 | 1466 | 277 | 107 | 107 |
| 1213 | 841 | 78 | 96 | 94 |
| 1214 | 602 | 202 | 89 | 89 |
| 1215 | 1056 | 115 | 102 | 101 |
| 1216 | 1000 | 219 | 52 | 51 |
| 1217 | 875 | 94 | 107 | 107 |
| 1218 | 1110 | 186 | 153 | 151 |
| 1219 | 999 | 85 | 95 | 87 |
| 1220 | 961 | 351 | 93 | 89 |
| 1221 | 1317 | 134 | 133 | 133 |
| 1222 | 1265 | 139 | 128 | 127 |
| 1223 | 1439 | 582 | 142 | 142 |
| 1224 | 1299 | 464 | 101 | 101 |
| 1225 | 873 | 127 | 81 | 78 |
| 1226 | 789 | 71 | 93 | 75 |
| 1227 | 882 | 61 | 81 | 78 |
| 1228 | 1009 | 117 | 61 | 28 |
| 1229 | 951 | 84 | 73 | 61 |
| 1230 | 1114 | 184 | 122 | 122 |
| 1231 | 1289 | 262 | 103 | 103 |
| 1232 | 1244 | 118 | 162 | 162 |
| 1233 | 804 | 159 | 109 | 99 |
| 1234 | 1176 | 293 | 64 | 64 |
| 1235 | 1138 | 112 | 97 | 92 |
| 1236 | 789 | 376 | 108 | 104 |
| 1237 | 1194 | 216 | 110 | 110 |
| 1238 | 781 | 307 | 82 | 68 |
| 1239 | 935 | 155 | 120 | 119 |
| 1240 | 1415 | 796 | 153 | 153 |
| 1241 | 1105 | 236 | 98 | 94 |
| 1242 | 1276 | 234 | 106 | 106 |
| 1243 | 1081 | 255 | 103 | 102 |
| 1244 | 983 | 139 | 151 | 151 |
| 1245 | 780 | 117 | 75 | 70 |
| 1246 | 996 | 96 | 167 | 165 |
| 1247 | 1035 | 200 | 172 | 169 |
| 1248 | 643 | 48 | 67 | 65 |
| 1249 | 1253 | 234 | 168 | 168 |
| 1250 | 1307 | 502 | 102 | 102 |
| 1251 | 824 | 71 | 103 | 101 |
| 1252 | 850 | 74 | 139 | 138 |
| 1253 | 986 | 280 | 128 | 128 |
| 1254 | 1027 | 354 | 161 | 161 |
| 1255 | 1204 | 738 | 144 | 141 |
| 1256 | 1576 | 314 | 145 | 144 |
| 1257 | 1873 | 407 | 164 | 164 |
| 1258 | 1002 | 182 | 194 | 193 |
| 1259 | 1020 | 185 | 141 | 141 |
| 1260 | 1154 | 208 | 353 | 353 |
| 1261 | 1262 | 404 | 308 | 308 |
| 1262 | 1078 | 179 | 152 | 152 |
| 1263 | 1072 | 174 | 242 | 242 |
| 1264 | 1025 | 157 | 99 | 61 |
| 1265 | 903 | 144 | 148 | 136 |
| 1266 | 1217 | 293 | 290 | 290 |
| 1267 | 1161 | 296 | 265 | 265 |
| 1268 | 1060 | 186 | 162 | 162 |
| 1269 | 1268 | 210 | 191 | 191 |
| 1270 | 1299 | 202 | 279 | 279 |
| 1271 | 1332 | 365 | 349 | 349 |
| 1272 | 431 | 130 | 171 | 115 |
| 1273 | 744 | 583 | 89 | 72 |
| 1274 | 1096 | 443 | 165 | 154 |
| 1275 | 424 | 128 | 159 | 155 |
| 1276 | 882 | 612 | 127 | 70 |
| 1277 | 1002 | 437 | 129 | 83 |
| 1278 | 1016 | 264 | 104 | 80 |
| 1279 | 912 | 440 | 107 | 98 |
| 1280 | 1017 | 179 | 163 | 163 |
| 1281 | 718 | 115 | 106 | 104 |
| 1282 | 586 | 142 | 111 | 82 |
| 1283 | 578 | 110 | 113 | 94 |
| 1284 | 408 | 226 | 84 | 68 |
| 1285 | 544 | 123 | 111 | 95 |
| 1286 | 681 | 340 | 111 | 84 |
| 1287 | 682 | 430 | 101 | 67 |
| 1288 | 525 | 124 | 89 | 77 |
| 1289 | 637 | 109 | 111 | 88 |
| 1290 | 540 | 136 | 94 | 26 |
| 1291 | 613 | 135 | 92 | 84 |
| 1292 | 632 | 151 | 90 | 54 |
| 1293 | 676 | 167 | 116 | 111 |
| 1294 | 506 | 118 | 95 | 50 |
| 1295 | 631 | 157 | 102 | 87 |
| 1296 | 699 | 119 | 86 | 85 |
| 1297 | 647 | 47 | 92 | 65 |
| 1298 | 803 | 146 | 92 | 92 |
| 1299 | 639 | 95 | 65 | 62 |
| 1300 | 718 | 68 | 70 | 66 |
| 1301 | 685 | 73 | 63 | 55 |
| 1302 | 765 | 71 | 79 | 68 |
| 1303 | 745 | 66 | 74 | 67 |
| 1304 | 759 | 129 | 98 | 97 |
| 1305 | 818 | 129 | 103 | 101 |
| 1306 | 853 | 103 | 93 | 82 |
| 1307 | 902 | 146 | 87 | 85 |
| 1308 | 801 | 115 | 86 | 85 |
| 1309 | 850 | 94 | 89 | 83 |
| 1310 | 757 | 59 | 97 | 92 |
| 1311 | 902 | 275 | 100 | 100 |
| 1312 | 848 | 111 | 103 | 68 |
| 1313 | 838 | 343 | 128 | 115 |
| 1314 | 842 | 85 | 94 | 86 |
| 1315 | 825 | 316 | 111 | 110 |
| 1316 | 874 | 60 | 120 | 115 |
| 1317 | 856 | 235 | 111 | 106 |
| 1318 | 853 | 168 | 92 | 81 |
| 1319 | 963 | 194 | 87 | 82 |
| 1320 | 877 | 88 | 100 | 76 |
| 1321 | 809 | 314 | 96 | 90 |
| 1322 | 863 | 149 | 127 | 123 |
| 1323 | 855 | 85 | 91 | 71 |
| 1324 | 769 | 258 | 101 | 97 |
| 1325 | 704 | 52 | 79 | 72 |
| 1326 | 710 | 66 | 94 | 92 |
| 1327 | 833 | 71 | 82 | 75 |
| 1328 | 843 | 207 | 73 | 73 |
| 1329 | 913 | 216 | 111 | 110 |
| 1330 | 910 | 107 | 78 | 64 |
| 1331 | 940 | 221 | 98 | 96 |
| 1332 | 690 | 151 | 144 | 122 |
| 1333 | 709 | 190 | 146 | 84 |
| 1334 | 413 | 101 | 146 | 137 |
| 1335 | 507 | 136 | 109 | 85 |
| 1336 | 399 | 14 | 120 | 89 |
| 1337 | 446 | 25 | 130 | 81 |
| 1338 | 451 | 99 | 102 | 90 |
| 1339 | 286 | 68 | 99 | 71 |
| 1340 | 803 | 147 | 91 | 84 |
| 1341 | 841 | 155 | 58 | 56 |
| 1342 | 650 | 80 | 77 | 64 |
| 1343 | 776 | 178 | 93 | 93 |
| 1344 | 741 | 129 | 85 | 73 |
| 1345 | 600 | 56 | 63 | 54 |
| 1346 | 721 | 55 | 96 | 96 |
| 1347 | 425 | 44 | 68 | 63 |
| 1348 | 523 | 26 | 105 | 100 |
| 1349 | 421 | 32 | 80 | 73 |
| 1350 | 577 | 52 | 57 | 50 |
| 1351 | 606 | 52 | 80 | 68 |
| 1352 | 356 | 20 | 73 | 60 |
| 1353 | 456 | 29 | 91 | 71 |
| 1354 | 682 | 80 | 118 | 65 |
| 1355 | 451 | 31 | 85 | 82 |
| 1356 | 294 | 48 | 62 | 58 |
| 1357 | 428 | 47 | 37 | 11 |
| 1358 | 423 | 42 | 59 | 51 |
| 1359 | 538 | 96 | 55 | 29 |
| 1360 | 902 | 137 | 101 | 91 |
| 1361 | 562 | 44 | 85 | 81 |
| 1362 | 483 | 54 | 109 | 83 |
| 1363 | 358 | 61 | 61 | 55 |
| 1364 | 347 | 25 | 79 | 78 |
| 1365 | 412 | 35 | 82 | 63 |
| 1366 | 831 | 53 | 89 | 87 |
| 1367 | 562 | 71 | 62 | 61 |
| 1368 | 477 | 39 | 71 | 69 |
| 1369 | 433 | 34 | 68 | 64 |
| 1370 | 372 | 17 | 63 | 59 |
| 1371 | 320 | 33 | 84 | 73 |
| 1372 | 417 | 21 | 73 | 59 |
| 1373 | 410 | 52 | 64 | 63 |
| 1374 | 686 | 85 | 83 | 77 |
| 1375 | 517 | 27 | 77 | 52 |
| 1376 | 431 | 68 | 85 | 33 |
| 1377 | 426 | 41 | 68 | 43 |
| 1378 | 379 | 31 | 78 | 64 |
| 1379 | 282 | 41 | 81 | 79 |
| 1380 | 871 | 155 | 156 | 74 |
| 1381 | 826 | 132 | 113 | 98 |
| 1382 | 944 | 152 | 227 | 227 |
| 1383 | 878 | 147 | 133 | 133 |
| 1384 | 806 | 188 | 130 | 108 |
| 1385 | 663 | 164 | 123 | 120 |
| 1386 | 344 | 78 | 91 | 68 |
| 1387 | 380 | 78 | 99 | 92 |
| 1388 | 694 | 171 | 113 | 97 |
| 1389 | 686 | 153 | 95 | 76 |
| 1390 | 1189 | 695 | 63 | 63 |
| 1391 | 880 | 145 | 104 | 103 |
| 1392 | 1083 | 104 | 98 | 94 |
| 1393 | 963 | 177 | 80 | 71 |
| 1394 | 907 | 140 | 108 | 106 |
| 1395 | 836 | 127 | 101 | 98 |
| 1396 | 867 | 165 | 99 | 85 |
| 1397 | 778 | 138 | 69 | 62 |
| 1398 | 763 | 135 | 92 | 85 |
| 1399 | 989 | 33 | 119 | 119 |
| 1400 | 930 | 175 | 105 | 103 |
| 1401 | 797 | 78 | 104 | 100 |
| 1402 | 949 | 173 | 100 | 98 |
| 1403 | 800 | 213 | 98 | 88 |
| 1404 | 873 | 167 | 87 | 67 |
| 1405 | 839 | 446 | 85 | 81 |
| 1406 | 378 | 117 | 133 | 101 |
| 1407 | 336 | 15 | 84 | 49 |
| 1408 | 420 | 17 | 94 | 90 |
| 1409 | 400 | 41 | 65 | 63 |
| 1410 | 506 | 34 | 64 | 59 |
| 1411 | 415 | 40 | 52 | 48 |
| 1412 | 544 | 83 | 67 | 48 |
| 1413 | 475 | 32 | 60 | 33 |
| 1414 | 336 | 39 | 58 | 25 |
| 1415 | 646 | 264 | 72 | 63 |
| 1416 | 213 | 34 | 87 | 70 |
| 1417 | 260 | 45 | 88 | 33 |
| 1418 | 351 | 158 | 63 | 38 |
| 1419 | 434 | 23 | 91 | 60 |
| 1420 | 342 | 41 | 107 | 50 |
| 1421 | 737 | 102 | 80 | 68 |
| 1422 | 404 | 35 | 72 | 69 |
| 1423 | 346 | 52 | 64 | 61 |
| 1424 | 372 | 53 | 108 | 50 |
| 1425 | 467 | 29 | 72 | 65 |
| 1426 | 439 | 63 | 66 | 65 |
| 1427 | 361 | 156 | 84 | 58 |