Table S 1: Table showing outcome of all convergence cycles for each step of refinement process of RT WO3 subgroup candidates. Every candidate was optimised within 1% of the minimum Rwp at least 9 separate times in the first step and 20 separate times in the second.

| Subgroup Number | Lattice Refinement Cycles | Number of times within 1% Rwp of minimum | Full Optimisation Cycles | Number of times with 1% Rwp of minimum |
| --- | --- | --- | --- | --- |
| 3 | 413 | 70 | 999 | 999 |
| 4 | 361 | 79 | 339 | 339 |
| 5 | 409 | 70 | 999 | 999 |
| 6 | 410 | 92 | 999 | 999 |
| 7 | 351 | 82 | 340 | 340 |
| 8 | 410 | 80 | 513 | 513 |
| 9 | 460 | 100 | 513 | 513 |
| 10 | 412 | 75 | 999 | 999 |
| 11 | 207 | 13 | 166 | 163 |
| 12 | 205 | 56 | 255 | 254 |
| 13 | 296 | 71 | 290 | 290 |
| 14 | 363 | 76 | 458 | 458 |
| 15 | 211 | 15 | 166 | 165 |
| 16 | 415 | 77 | 505 | 505 |
| 17 | 183 | 18 | 211 | 209 |
| 18 | 211 | 55 | 238 | 237 |
| 19 | 430 | 93 | 398 | 398 |
| 20 | 408 | 80 | 999 | 999 |
| 21 | 414 | 76 | 999 | 999 |
| 22 | 323 | 65 | 169 | 169 |
| 23 | 274 | 63 | 145 | 145 |
| 24 | 295 | 66 | 348 | 348 |
| 25 | 428 | 91 | 406 | 406 |
| 26 | 312 | 71 | 168 | 168 |
| 27 | 435 | 69 | 389 | 389 |
| 28 | 313 | 72 | 166 | 166 |
| 29 | 275 | 62 | 150 | 150 |
| 30 | 515 | 457 | 1486 | 1486 |
| 32 | 522 | 468 | 1488 | 1488 |
| 33 | 368 | 57 | 402 | 402 |
| 34 | 453 | 105 | 627 | 627 |
| 35 | 406 | 75 | 999 | 999 |
| 36 | 357 | 60 | 236 | 236 |
| 37 | 241 | 46 | 146 | 146 |
| 38 | 294 | 66 | 284 | 284 |
| 39 | 334 | 75 | 399 | 399 |
| 40 | 356 | 67 | 238 | 238 |
| 41 | 354 | 68 | 400 | 400 |
| 42 | 335 | 79 | 314 | 314 |
| 43 | 244 | 52 | 156 | 156 |
| 44 | 362 | 89 | 304 | 304 |
| 45 | 389 | 84 | 520 | 520 |
| 46 | 338 | 50 | 331 | 331 |
| 47 | 338 | 69 | 336 | 336 |
| 48 | 430 | 85 | 528 | 528 |
| 49 | 254 | 62 | 147 | 147 |
| 50 | 343 | 72 | 322 | 322 |
| 51 | 311 | 63 | 197 | 197 |
| 52 | 421 | 71 | 429 | 429 |
| 53 | 366 | 81 | 253 | 253 |
| 54 | 192 | 80 | 220 | 220 |
| 55 | 225 | 58 | 163 | 156 |
| 56 | 400 | 62 | 419 | 419 |
| 57 | 314 | 75 | 199 | 199 |
| 58 | 242 | 61 | 201 | 191 |
| 59 | 80 | 11 | 240 | 239 |
| 60 | 142 | 17 | 252 | 252 |
| 61 | 240 | 68 | 245 | 239 |
| 62 | 259 | 59 | 148 | 148 |
| 63 | 217 | 44 | 141 | 141 |
| 64 | 265 | 54 | 311 | 311 |
| 65 | 237 | 64 | 172 | 172 |
| 66 | 172 | 63 | 221 | 221 |
| 67 | 96 | 13 | 245 | 244 |
| 68 | 364 | 76 | 306 | 306 |
| 69 | 243 | 59 | 171 | 171 |
| 70 | 192 | 83 | 238 | 238 |
| 71 | 104 | 9 | 246 | 245 |
| 72 | 152 | 25 | 254 | 254 |